## Slide 1: Fracture properties of welded 304L in hydrogen environments
Joe Ronevich, Chris San Marchi, Michael Maguire, Dorian K. Balch
2021 International Conference on Hydrogen Safety (ICHS)
September 21-24, 2021
SAND2021-11145C
Sandia National Laboratories

## Slide 2: Motivation – Welds offer benefits compared to mechanical joints  Fracture behavior in hydrogen is not well defined
Austenitic stainless steels are more resistant to H2 embrittlement
     Desirable for H2 containment components
Commonly assumed that welds are more susceptible than base metal
 Weld usage has been limited due to lack of data
Significant benefits for using welding compared to mechanical joints
  Lower cost
  Less maintenance
  Reduced leaks (safety and product loss)
In some applications (e.g. large pressure vessels), necessary to use welds
Fracture properties of stainless steel welds in H2 environments are limited

## Slide 3: Electron beam (EB) welds have advantages over conventional welds like GTA welds
Electron beam welds
Reduced heat input
Smaller heat-affected zone (HAZ)
Maintain higher strength
No filler wire
Gas Tungsten Arc (GTA) Weld
Requires filler metal
Prep can be easier in field
Forged 304L

## Slide 4: Extracted test coupons from EB weld rings for fracture testing
Arc coupons from forgings were tested for comparison
304L Forging
YS = 447 MPa
UTS = 666 MPa

## Slide 5: Thermally precharged samples to represent long-term exposure to hydrogen
Diffusion rates at room temperature in austenitic stainless steel are very slow (10-16 m2/s)
  ~ 1 mm in 16 years
Use thermal precharging to accelerate diffusion and permit saturation of material with hydrogen
  573 K at 138 MPa for ~ 10 days = 140 wppm H
  573 K at 41 MPa for ~ 10 days = 66 wppm H
    Hydrogen contents were measured from an outside laboratory on coupons extracted from samples
  Samples were then stored at 220 K until testing in air
Two different internal hydrogen contents were evaluated which represent different long term hydrogen exposures

## Slide 6: Mechanical testing performed in air on H-precharged samples at 223 K (-50°C) and 293 K (20°C)
Low temperatures (223 K) are known to degrade fracture properties of stainless steels and gas is often prechilled to these temperatures at hydrogen refueling stations
Tensile Testing
  Displacement rate = 5 x 10-4 s-1
  Measurements of yield strength, tensile strength and reduction of area (RA)
Fracture testing
  Elastic-plastic fracture testing according to ASTM E1820 using constant rising displacement
  Displacement rate = 1.5 mm/hr
  JH value determined by intersection of J vs crack extension (Da) (e.g. J-R) curve with 0.2 mm construction line

## Slide 7: Ductility loss of H-precharged forgings and EB welds
0 wt ppm
293 K
RA ~ 0.85
66 wt ppm
293 K
RA ~ 0.53
140 wt ppm
223 K
RA ~ 0.22
Reduction of area decreased with increasing hydrogen content
Fracture surfaces of tensile samples
Decreasing ductility

## Slide 8: Fracture resistance (JH) decreased with increasing internal hydrogen content
Forged 304L and EB welds, similarly, exhibited decreasing fracture resistance as internal hydrogen content increased
Low temperature further degraded fracture performance in both weld and forging
For reference:
Many pressure vessels
(Cr-Mo) steels
have JH ~ 10 to 20 kJ/m2
in 100 MPa H2 gas at 293K
EB weld fracture behavior was similar to forged 304L

## Slide 9: Fracture resistance of EB weld compared to conventional Gas Tungsten Arc (GTA) welds
EB weld has superior fracture resistance to GTA welds (304L/308L) from literature1,2 at room temperature (293 K)
At low temperature (223 K), the fracture resistance is comparable between EB and GTA welds
Small fractions of ferrite are present in all welds, which is likely cause for reduced performance at 223 K
1Ronevich, J. (PVP2019-93823)
2Jackson, H. (Corr Science, 2013)
Low temperature appears to result in similar fracture behavior among welds

## Slide 10: Crack deflection improves fracture resistance in EB weld
Crack branching is observed
Cracks growth along elongated features
Crack growth direction
EB weld
GTA weld
Orientation and finer features result in crack deflection and improved fracture resistance in EB
140 wppm H

## Slide 11: Summary
Tensile and fracture coupons were extracted from forged 304L and Electron beam (EB) welded 304L, thermally precharged with hydrogen (66 or 140 wppm H), and tested at 293 K or 223 K
Reduction of Area (RA) measurements were consistent between forged 304L and EB weld
  Both decreased with increasing internal H-content
  Both decreased with decreasing temperature
Fracture resistance degraded with increasing H-content for both forged 304L and EB weld
  Low temperature reduced fracture resistance (JH)
EB welds outperformed conventional gas tungsten arc (GTA) welds at 293 K but had similar JH values at 223 K
  Improved performance of EB weld at 293 K is attributed to crack deflection brought about by finer microstructure and microstructure orientation
Overall, EB weld performance with hydrogen was comparable to forged 304L suggesting it could be a viable, cost-effective replacement to mechanical joints

## Slide 12: Acknowledgements / Questions
Special thanks to Jeff Campbell for thermal hydrogen precharging and James McNair for sample preparation at Sandia and the whole Hydrogen Effects of Materials Laboratory (HEML) Team.
Sandia National Laboratories is a multimission laboratory managed and operated by National Technology and Engineering Solutions of Sandia, LLC., a wholly owned subsidiary of Honeywell International, Inc., for the U.S. Department of Energy’s National Nuclear Security Administration under contract DE-NA-0003525. This paper describes objective technical results and analysis. Any subjective views or opinions that might be expressed in the paper do not necessarily represent the views of the U.S. Department of Energy or the United States Government.
Joe Ronevich
jaronev@sandia.gov