## Slide 1: Effect of microstructural and environmental variables on ductility of austenitic stainless steels
Chris San Marchi,
Sandia National Laboratories
Joe Ronevich, Julian Sabisch, Josh Sugar, Doug Medlin (Sandia)
Brian Somerday (Somerday Consulting, LLC)
Sandia National Laboratories is a multimission laboratory managed and operated by National Technology and Engineering Solutions of Sandia, LLC., a wholly owned subsidiary of Honeywell International, Inc., for the U.S. Department of Energy’s National Nuclear Security Administration under contract DE-NA-0003525.
Funding partially provided by the Safety, Codes and Standards subprogram of the Fuel Cell Technologies Office of the Office of Energy Efficiency and Renewable Energy for the U.S. Department of Energy.
SAND2019-10874 C

## Slide 2: H-Mat – Hydrogen Materials Compatibility Consortium:
H-Mat addresses the challenges of hydrogen degradation by elucidating the mechanisms of hydrogen-materials interactions with the goal of providing science-based strategies to design materials (micro)structures and morphology with improved resistance to hydrogen degradation.
Six new projects with universities and industry currently being negotiated with DOE for inclusion under the H-Mat umbrella
Science-based advancement of materials for hydrogen technologies

## Slide 3: H-Mat approach: integrate innovative computational & experimental activities across length scales

## Slide 4: Microstructural and environmental variables are considered in this study
Microstructural variables
  Composition
    304L – 316L (nickel)
    XM-11 (nickel-manganese)
  Alloy stability
    Metastable (304L, 316L)
    Stable (XM-11)
  Strength
    Forged – Annealed (XM-11)
Environmental variables
  Hydrogen concentration
    0 to 140 wt ppm H (to 220 wt ppm H in XM-11)
  Temperature
    Room temperature (293 K) and low temperature (223K)
Environment
Stress / Mechanics
Materials
Hydrogen embrittlement occurs in materials under the influence of stress in hydrogen environments

## Slide 5: Austenitic stainless steels in this study
Designation | Fe | Cr | Ni | Mn | Mo | Si | C | N | S | P
304L - F | Bal | 19.6 | 10.6 | 1.6 | – | 0.65 | 0.028 | 0.04 | 0.0042 | 0.02
316L - F | Bal | 16.7 | 12.7 | 0.64 | 2.8 | 0.62 | 0.020 | 0.04 | 0.0023 | 0.008
XM-11 - F | Bal | 21.1 | 7.2 | 9.1 | ­– | 0.53 | 0.031 | 0.28 | 0.001 | 0.015
XM-11 - A | Bal | 19.3 | 6.8 | 9.0 | – | 0.39 | 0.022 | 0.25 | <0.001 | 0.017
F= forged; A = annealed
Designation |  | Yield Strength (MPa) | Tensile Strength (MPa) | Elongation (%) | Reduction of Area (%)
304L - F | Metastable | 436 | 611 | 69 | 85
316L - F | Metastable | 422 | 571 | 70 | 84
XM-11 - F | Stable | 674 | 830 | 48 | 76
XM-11 - A | Stable | 457 | 755 | 65 | 83

## Slide 6: H-precharging is used to simulate hydrogen service environment
Thermal H-precharging
  Exposure to gaseous hydrogen until specimen is saturated with hydrogen
    Pressure: varied to achieve target [H] (up to 138 MPa)
    Temperature: 300˚C
Testing in air after precharging with hydrogen
Mechanical testing in H-precharged condition (internal H) is similar to in situ testing in high-pressure gaseous hydrogen (external H) for tension, fatigue and fracture
Conditions simulate the high concentration anticipated under high triaxial stress (i.e., near crack tip) in gaseous hydrogen

## Slide 7: Tensile stress-strain curves show similar behavior for all materials in general
Elongation
Type 304L shows the lowest elongation to failure
Low temperature has the greatest effect on tensile elongation of 304L
Strength
Temperature seems to have a greater effect on strength properties of XM-11 compared to 304L and 316L
In general, temperature strengthens austenitic stainless steels
  Exception: Type 304L

## Slide 8: Tensile stress response roughly scales with hydrogen concentration for type 304L
Hydrogen acts similar to a solid-solution strengthening element
Hydrogen substantially reduces tensile ductility in 304L
  At low temperature, reduction of ductility results in decreased tensile strength

## Slide 9: Tensile stress response roughly scales with hydrogen concentration for type 316L
Hydrogen acts similar to a solid-solution strengthening element
Hydrogen has modest effect on tensile ductility
  At low temperature, tensile ductility remains high and tensile strength with hydrogen is greater than without hydrogen

## Slide 10: Yield strength increases approximately linearly with hydrogen concentration for types 304L & 316L
Low temperature reduces yield strength of 304L while strength of 316L increases at low temperature
Effect of hydrogen concentration, however, remains constant
304L
316L

## Slide 11: Compositional effects are not straight forward when both stable and metastable alloys are considered
All materials show a substantial loss of ductility with high concentration of hydrogen
H-precharging reveals that even high-Ni 316L shows substantial loss of ductility
Metastable 304L and stable XM-11 show similar loss of ductility
  Despite much lower nickel content of XM-11
304L/316L: 140 H
XM-11: 220 H

## Slide 12: Ductility loss is nominally a linear function of hydrogen concentration for type 304L & 316L
‘Offset’ of ductility with hydrogen depends on composition and temperature (i.e., extrapolated value of RA)
Dependence on hydrogen concentration (‘slope’) is similar for type 304L at both temperatures and type 316L at room temperature
Slope of ductility loss with hydrogen concentration is significantly greater for type 316L at low temperature
  Results suggest that high-Ni 316L is not as resistant to hydrogen as generally assumed

## Slide 13: Strain-induced a’-martensite transformation in metastable austenitic stainless steels depends on composition
304L: 10.6% Ni
316L: 12.7% Ni

## Slide 14: Strain-induced a’-martensite transformation in 304L

## Slide 15: Strain-induced a’-martensite transformation in 304L
At low volume of transformation, hydrogen promotes strain-induced transformation

## Slide 16: Strain-induced a’-martensite transformation in 304L
At high volume of transformation, hydrogen suppresses strain-induced transformation

## Slide 17: Strain-induced a’-martensite transformation in 316L

## Slide 18: Strain-induced a’-martensite transformation in 316L
At low volume of transformation, hydrogen promotes strain-induced transformation

## Slide 19: Ductility loss in austenitic stainless steels with internal hydrogen does NOT correlate with a’-martensite
3% a’- martensite
14% a’-martensite
11% a’-martensite

## Slide 20: Ductility loss in austenitic stainless steels with internal hydrogen does NOT correlate with a’-martensite
Low ductility with hydrogen is observed in both stable and metastable alloys
Moderate ductility with hydrogen is observed with both low and high martensite transformation
Promotion of martensite formation at low martensite content is likely related to greater nucleation sites due to hydrogen-promoted planar slip
Suppression of martensite formation at high martensite content is likely related to stabilization of austenite by interstitial hydrogen

## Slide 21: Summary and conclusions
Internal H strengthens alloys approximately linearly with hydrogen content
Internal H reduces tensile ductility
  Temperature reduces RA by about the same amount for all alloys
Internal H promotes strain-induced a’-martensite when volume of martensite is small (<20%)
Internal H suppresses strain-induced a’-martensite when volume of martensite is large (>20%)
No apparent correlation between a’-martensite and ductility with internal H
Hydrogen has strong effects on ductility of all stainless steels (which are not always captured by tests in external H)
Hydrogen-assisted fracture cannot be understood by hydrogen-induced fracture of strain-induced martensite