## Slide 1: Hydrogen Research Priority Workshop Hydrogen & Fuel Cell Vehicles Global Technical Regulation
Nha Nguyen
U.S. Department of Transportation
National Highway Traffic Safety Administration

## Slide 2: Background
In 2009, The U.S., Japan and Germany co-sponsored a working group to develop a Global Technical Regulation (GTR) Under the United Nations 1998 Agreement.
The working group consisted of governments participants from China, European Union, Korea, Canada and India; and industry participants from standard organizations, automobile and component manufacturers
In June 2013, Phase 1 was completed, establishing GTR No. 13: Contracting Parties under the 1998 Agreement are obligated to start an adoption process of GTR No.13 into their national regulations
http://www.unece.org/trans/main/wp29/wp29wgs/wp29gen/wp29glob_registry.html

## Slide 3: Compresses Hydrogen Fuel Cell Vehicle
    High pressure fuel container system
    Fuel system at vehicle level: in-use and post-crash hydrogen leakage limits
    Electrical integrity of high voltage system: in-use and post-crash

## Slide 4: Verification test for Baseline Metrics
Baseline Initial Burst Pressure Test
  Burst pressure within ±10% of BP0
  Burst pressure ≥ BPmin of 225% NWP
Baseline Initial Pressure Cycling Test
  Pressure cycle for 22,000 cycles without rupture

## Slide 5: Verification Test for Performance Durability (Sequential hydraulic cycling tests)
Number of cycles is specified by individual contracting party (5,500, 7,500 and 11,000)
Proof pressure test
Drop (impact) test
Surface damage
Chemical exposure
ambient temperature pressure cycling tests
High temperature static pressure test
Extreme temperature pressure cycling
Residual proof pressure test (180% NWP for 4 mins)
Residual strength burst test (within 20% of BPo)
180% NWP
(4 min)

## Slide 6: Verification Test for On-Road Performance (Sequential pneumatic/hydraulic cycling tests)
Number of cycles: 500
Proof pressure test
Ambient and extreme temperature gas pressure cycling test (pneumatic)
Extreme temperature static gas pressure leak/permeation test (pneumatic)
Residual proof test (180% NWP for 4 mins)
Residual strength burst test (hydraulic) – Within 20% of BPo
180% NWP
(4 min)

## Slide 7: Combining Localized and Engulfing Fire
A hydrogen storage system is pressurized to NWP and exposed to fire. A temperature-activated pressure relief device shall release the contained gases in a controlled manner without rupture.

## Slide 8: Fire Test Profile
1
600o C
800o C
Localized Fire Exposure
Engulfing Fire
Minutes
13
11
300o C
3
Min
Temp
Localized Area
Engulfing Region Outside Localized Area (burner ramp rate)
Ignite
Main
Burner
0

## Slide 9: Fuel System Requirements
Fuel System Integrity:
  Fuel Receptacle and Label requirements
  PRD requirements
  Exhaust requirements
In-use fuel leakage:
  Warning tell-tale at 2±1% of Hydrogen concentration in enclosed spaces
Post-crash leakage:
  Less than 3±1% of Hydrogen concentration in enclosed spaces

## Slide 10: Electrical Safety
In-Use requirements:
  Protection from high voltage shock
    Absence of high voltage
    Isolation resistance
    Barrier
    label
  Isolation resistance monitoring system
  Functional safety
Post-crash requirements:
  Protection from high voltage shock
  Battery leakage and retention

## Slide 11: Status of GTR Adoption
Adopted:
  EU transposed GTR into UN-ECE
  Japan
  Korea
The U.S. is currently preparing a notice of proposed rulemaking (NPRM):
  Completed a series of fuel tank tests to validate the test procedures
  NPRM is expected in 2017

## Slide 12: GTR Phase 2
Phase 2 GTR is expected to start early 2017
  Material compatibility
  Stress rupture
  Electric safety
  Improve current test procedures
  Potential scope revision to include other vehicle classes

## Slide 13
http://www.nhtsa.gov/
nha.nguyen@dot.gov
Questions

## Slide 14: HFCV GTR No. 13 Hydrogen Research priority workshop